## Slide 1: HK Cross Ocean Technology Ltd
PCB process capability table

## Slide 2
Process | Item | Illustration | Standard process capability | Advanced process capability
Board cut | Material |  | FR4 Aluminum PTFE Ceramic HDI | FR4 Aluminum PTFE Ceramic HDI
 | board thickness | a | Inner Core：T ≥0.3mm Thickness of finished outer layer：0.45mm≦T≦3.2mm Board thickness tolerance： | Inner Core：T ≥0.2mm Thickness of finished outer layer：0.35mm≦T≦3.2mm Board thickness tolerance:
 | copper thickness | a | Inner copper thickness：≦4oz Outer copper thickness：≦4oz | Inner copper thickness：≦6oz Outer copper thickness：≦6oz
 | panel size | a b | Max Size：520*622mm Min Size：200*310mm | Max Size：520*622mm Min Size：200*310mm
 | Plating clip edge area | a b | a：Double-sized：≥8mm a: Multilayer：≥12mm b:Non-plated clip edge：≥ 6mm | a：Double-sized：≥8mm a: Multilayer：≥12mm b:Non-plated clip edge：≥ 6mm
Board thickness | Tolerance
1.0mm以下 | ±10%
1.0mm以上 | ±0.1mm
Board thickness | Tolerance
1.0mm以下 | ±10%
1.0mm以上 | ±0.1mm

## Slide 3
Process | Item | Illustration | Standard process capability | Advanced process capability
Inner layer Lamination | Layer |  | 2-8 layers | 16 layers
 | Inner layer minimum line width Line spacing | w s |  | 
 | Media layer thickness |  | Min：0.076mm Max：0.6mm:over 0.6mm needs to add board | Min：0.076mm Max：0.6mm:over 0.6mm needs to add board
 | Distance from inner layer hole to line | a | a≥10mil | a≥8mil
 | Minimum isolation ring | a a aa | a≥8mil | a≥6mil
 | Inner smallest hole ring | a | a≥6mil | a≥5mil
 | Interlayer Alignment |  | Deviation≦ 3mil | Deviation≦ 3mil
基材铜厚 | 原稿 | 工作稿
HOZ | 4/4mil | 5/3mil
1OZ | 5/5mil | 6/4mil
2OZ | 6/6mil | 8/4mil
3OZ | 8/8mil | 12/4mil
基材铜厚 | 原稿 | 工作稿
HOZ | 4/3mil | 4/3mil
1OZ | 5/4mil | 6/3mil
2OZ | 5/5mil | 6.5/3.5mil
3OZ | 6/6mil | 8/4mil
a

## Slide 4
Process | Item | Illustration | Standard process capability | Advanced process capability
Drilling | Hole Diameter |  | Min hole diameter：0.25mm Max hole diameter：6.3mm | Min hole diameter：0.2mm
 | Hole accuracy | designed hole in fact hole | ±3mil | ±3mil
 | Hole edge to hole edge distance | a | a≥12mil | a≥10mil
 | Hole diameter tolerance |  | PTH hole：±3mil NPTH hole: ±2mil | PTH hole： ±2mil NPTH hole: ±1.5mil
 | Min SLOT |  | 0.7mm | 
 | Two-drill bit accuracy |  | Deviation≦4mil | 
 | Countersunk mechanical holes | R T H D | Hole diameter：±4mil R Drill angle： 90-165° H Remaining thickness tolerance：±8mil T Depth Tolerance：±8mil | Hole diameter：±4mil R Drill angle： 90-165° H Remaining thickness tolerance：±8mil T Depth Tolerance：±8mil
 | Hole wall roughness | C | C：≦1mil | C：≦1mil

## Slide 5
Process | Item | Illustration | Standard process capability | Advanced process capability
Electroplating | Backlighting |  | ≥9 Level | ≥9 Level
 | Max Aspect Ratio | H A Aspect Ratio=H/A | 6:1 | 8:1
 | Copper plating thickness |  | ≥18um（according to requirement） | ≥18um（according to requirement）
 | Uniform plating capability |  | ≥85% | ≥85%
 | Depth Capability |  | ≥85% | ≥85%

## Slide 6
估计 钻孔后长：42.3～44mil
比PE设计偏短达：6.7~9mil
Process | Item | Illustration | Standard process capability | Advanced process capability
Circuit | Alignment accuracy |  | ±3mil | ±2mil
 | Line width/Line space | W S |  | 
 | Single-sided minimum hole ring | a |  | 
 | Hole masking capability |  | Round Hole：6.0mm， Slot Hole：4*3.0mm single-sided ring：≧6mil | Round Hole：6.0mm， Slot Hole：4*3.0mm single-sided ring：≧5mil
 | Minimum distance from the line to the edge of the formed hole | a NPTH Hole | ≥10mil | ≥8mil
Copper thickness | Workpiece line width/line spacing
HOZ | 5/4mil
1OZ | 6/5mil
2OZ | 8/5mil
Copper thickness | Workpiece line width/line spacing
HOZ | 4/3mil
1OZ | 5/4mil
2OZ | 6/4mil
Copper thickness | Part Holes | Conductive holes
HOZ | ≥6mil | ≥5mil
1OZ | ≥7mil | ≥6mil
2OZ | ≥8mil | ≥7mil
Copper thickness | Part Holes | Conductive holes
HOZ | ≥5mil | ≥4mil
1OZ | ≥6mil | ≥5mil
2OZ | ≥8mil | ≥7mil

## Slide 7
Process | Item | Illustration | Standard process capability | Advanced process capability
Etching | Etching factor |  | Etching factor =D/C C=(A-B)/2 ≥3.5 | Etching factor =D/C C=(A-B)/2 ≥3.5
 | Etched text line width | b a |  | 
 | BGA size |  | Min BGA：0.25mm HASL Min BGA：0.3mm | Min BGA：0.25mm HASL Min BGA：0.3mm
 | Line width control |  | ±15% | ±10%
A
B
C
抗蚀层
基材
铜线路
D
Copper thickness | text width a | text height b
HOZ | ≥8mil | ≥30mil
1OZ | ≥10mil | ≥35mil
2OZ | ≥12mil | ≥40mil
B
Copper thickness | text width a | text height b
HOZ | ≥8mil | ≥30mil
1OZ | ≥10mil | ≥35mil
2OZ | ≥12mil | ≥40mil

## Slide 8
Process | Item | Illustration | Standard process capability | Advanced process capability
Soldering | Alignment accuracy |  | ±3mil | ±3mil
 | Non-Tented via/Exposed Via |  | ≥4mil BGA：2mil SMD:3mil | ≥2.5mil BGA：1.5mil SMD:2.5mil
 | Minimum oil bridge width | a |  | 
 | Solder resist side corrosion amount | a |  | 
 | Minimum distance from exposed via to line | a | 3mil | 2.5mil
 | Minimum lower oil grid | a |  | 
 | Hole plugging capacity |  | Board thickness1.6mm，Maximum plug hole drill nozzle：0.7mm（thickness/drill nozzle≥2.5） | Board thickness1.6mm，Maximum plug hole drill nozzle：0.7mm（thickness/drill nozzle≥2.5）
Copper | S/M | Others
HOZ | 4mil | 5mil
1OZ | 5mil | 7mil
2OZ | 6mil | 8mil
Solder color | Side erosion amount
Green | 1mil
White | 1.5mil
Black | 1.5mil
Copper | Grid width
HOZ | ≥6mil
1OZ | ≥8mil
2OZ | ≥10mil
Copper | S/M | Others
HOZ | 4mil | 5mil
1OZ | 5mil | 7mil
2OZ | 6mil | 8mil
Solder color | Side erosion amount
Green | 1mil
White | 1.5mil
Black | 1.5mil
Copper | Grid Width
HOZ | ≥6mil
1OZ | ≥8mil
2OZ | ≥10mil

## Slide 9
Process | Item | Illustration | Standard process capability | Advanced process capability
Silk screen Carbon Oil | silk screen size | Height a Width b |  | 
 | Silk screen accuracy | 6mil 6mil | ±6mil | ±5mil
 | Min distance from Carbon Oil to circuit PAD | a | ≥12mil | ≥10mil
 | Carbon Oil Space | a | ≥18mil | ≥15mil
B
Copper | legend heighta | legend widthb
HOZ | 32mil | 5mil
1OZ | 40mil | 6mil
2OZ | 48mil | 8mil
Copper | legend heighta | legend widthb
HOZ | 32mil | 5mil
1OZ | 40mil | 6mil
2OZ | 48mil | 8mil

## Slide 10
Process | Item | Illustration | Standard process capability | Advanced process capability
Forming | space from hole to edge | a | ≥10mil | ≥8mil
 | space from circuit to forming edge | a |  | 
 | Forming accuracy | a b | ±4mil | ±4mil
 | min via diameter | Ø | Ø ≥2.0mm | Ø ≥2.0mm
 | Min R angle |  | 0.2mm | 0.2mm
 | via tolerance |  | ±4mil | ±4mil
Single/Duoble-sided | 8mil
4 Layers | 10mil
over 4 layers | 12mil
Single/Duoble-sided | 8mil
4 layers | 10mil
over 4 layers | 12mil

## Slide 11
Process | Item | Illustration | Standard process capability | Advanced process capability
V-CUT | V-CUT Angle | R | R: 30° 45° 60° | R:30° 45° 60°
 | V-CUT Registration | a | ±4mil | ±4mil
 | V-CUT left thickness | H | 0.3mm(or special requirements） | 0.3mm（or special requirements）
 | left thickness tolerance |  | ±4mil | ±4mil
 | Min V-CUT board thicness |  | 0.6mm | 0.6mm

## Slide 12
Process | Item | Illustration | Standard process capability | Advanced process capability
Surface finish | HASL LF | No |  | 
 | HASL | No |  | 
 | ENIG | No |  | 
 | Chemical silver plating | No | Chemical Silver Thickness：0.2-1.0um | Chemical Silver Thickness：0.2-1.0um
 | OSP | No | OSP thickness:0.25-0.5um OSP Min Board size：70*70mm | OSP thickness:0.25-0.5um OSP Min Board size：70*70mm
Tin spray thicness | 0.05-1.5mil
Tin spray times | ≦2 times
Chemical tin thickness | 1-2um
chemical tin times | ≦2 times
Chemical nickel thicness | 3-8um
Chemical gold thickness | 0.025-0.075um
Tin spray thicness | 0.05-1.5mil
Tin spray times | ≦2 times
Chemical tin thickness | 1-2um
chemical tin times | ≦2 times
Chemical nickel thicness | 3-8um
Chemical gold thickness | 0.025-0.075um

## Slide 13
Process | Item | Illustration | Standard process capability | Advanced process capability
Test | test size |  | Dedicated machine：max：330*430mm Flying Needle Machine：max：622*546mm Dedicated machine：min：100*100mm Flying Needle Machine：min:20*40mm | Dedicated machine：max：330*430mm Flying Needle Machine：max：622*546mm Dedicated machine：min：100*100mm Flying NeedleMachine：min:20*40mm
 | min test space |  | 0.075mm | 0.075mm
 | Min test PAD |  | 0.2mm | 0.2mm
 | Maximum number of test points for dedicated machines |  | 6144 points | 6144 points